SUMMER PROJECT

ON

EFFECT OF COLD WORK IN CORROSION AND MICROSTRUCTURE OF 304 STAINLESS STEEL

Submitted by:

Ashika Agrawal

Metallurgical& Materials Engineering Department

NIT, ROURKELA

Acknowledgement

I am very much thankful to Prof. S.C Mishra, HOD, for recommend me and indebted to Dr.P.Ramarao for selecting me to avail the summer internship with financial assistance to undertake summer internship at BARC Mumbai, Mumbai. I would like to thank Bhabha Atomic Research Centre, Mumbai for providing me   the opportunity to this internship during May-July 2015. I would also like to thank Dr V.Kain and Dr.A.Parag, my guide, for not only providing me with this project but also trusting me to see the project to the end by ourselves and for guiding every time. I would like to thank Dr Abhijit Ghosh for helping us with the SEM images.

Ashika Agrawal

Contents

- Introduction...……………………………………………………4

- Experimental  procedure……………………………….....5

- Results and Discussions……………...............................7

- Conclusions………………………………………………….……18

- References………………………………………………….……..20

Introduction

Type 304 stainless steel is a T300 series austenitic stainless steel .It contains minimum of 18% Chromium , 8% Nickeland maximum of 0.08% carbon .It is defined as a Cr-Ni austenitic alloy. It is18/8 grade stainless steel used in pans and cookery tools. It has excellent toughness, ease of cleaning, fabrication and beauty of appearance.

The chemical compositions of SS304 were determined by XRFListed in table 1.

SS304 Chemical Composition

| Element | C | Cr | Ni | Mn | Si | P | S |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Weight % | 0.054 | 18.10 | 8.20 | 1.02 | 1.10 | 0.035 | 0.006 |

Table-1

Lower carbon minimizes chromium carbide (Cr23C6) precipitation at the grain boundaries due to welding and its susceptibility to intergranular corrosion. It is also represented by UNS S30400.(UNS stands for unified numbering system listed in metals and alloys).It has good corrosion /oxidation resistance, its low temperature property responding well to hardening by cold work. Many corrosion experiments were conducted in different standard solutions to know its susceptibility to intergranular corrosion and stress corrosion cracking. Single loop electrochemical polarization reactivation(SL-EPR)  and double loop electrochemical polarization reactivation (DL-EPR) tests were conducted to know the stability of passive film and regions of chromium depletion at grain boundary.Martensite structure was also clearly observed under optical and scanning electron microscope.

EXPERIMENTAL PROCEDURE:

1.The Martensitic Transformation:

The as-received sample of type 304 stainless steel with initial thickness of 2.87mm was in the form of rectangular plate  was cut into 4 pieces .The sample was then rolled/deformed uniaxially to reduced the thickness to 20%,40%, 60% of the initial thickness using rolling machine (notation  CW00,CW20,CW40,CW60).

2.% OF MARTENSITE CONTENT:

The magnetic character of type 304 stainless steel was measured in terms of % martensite content using feritscope after cold rolling.

3.Micro hardness Test:

A sample of stainless steel was spot welded on one side of the specimen, and the wire was covered by an insulated sleeve. The samples were then mounted in a cold setting resin. The mounted samples were wet ground on successively finer grit of emery papers from 80 to 1200 grit. The final polish was done using diamond paste (1µm) on a polishing cloth. Then ultrasonic cleaning was done using 3 to 4 drops of soap solution in distilled water for 5 to 6 minutes and then the samples were rinsed with distilled water and dried using drier.

The samples were electrolytic ally etched in 10%Oxalic acid (H2C2O4) at 10V for 90s. The microstructure were observed using optical microscope at different magnification such as 100x, 200x, 500xand recorded. Micro hardness was taken using high load micro hardness tester at 300gf and dwell time of 15 seconds.

Micro hardnesswas also taken in low load micro hardness tester at 100mN, 300mN, 500mN, 700mNforce and dwell time 20s and creep 5s.

4. POTENTIODYNAMIC TEST:

The samples were again polished to remove the indents formed during hardness test or else take  unpolished  samples drilled a 2mm diameter hole on one side of each samples .The specimens were grounded on successively finer grit of emery paper to 1200 grit. The edges and corners were polished. Then the whole samples were diamond polished using 1µm diamond paste .The specimen and a stainless steel wire was used to provide electrical contact. The connecting wire was covered by an insulated sheathing and the contact surface between the specimen and the curve were covered using a polytetrafluoroethylene(PTFE) tape,except a square area all other surfaces were covered with a liquor .The liquor used was generally a thick nail paint .The polarization curves were generated using a portable field potentiostat.

The experiments were carried out at room temperature. Before the electrochemical experiments, the surface of the sample was exposed to cathodic cleaning at -0.9 VSCE for 60s to reduce the air formed oxide film. Different solutions were prepared using the standard combination of H2SO4 and KSCN as activator. The solutions were deaerated using argon gas in a closed corrosion vessel for 45minutes. The solutions were then used as the test solution. The sample was the working electrode, the platinum electrode as the counter electrode and saturated calomel electrode (SCE) as the reference electrode.

Then the anodic polarization was carried out and the potential was kept from -0.05V to 1.2V.The potential scan rate used was 2mV/sec.

After the completion of the test, the specimens were washes with distilled water and examined under optical microscope to determine the type and extend of corrosion .Optical microscope enables only those details of the structure to be observed, that are larger than 0.15-0.2 microns.

MICROSTRUCTURE ANALYSIS IN BERAHA’S ETCHANT USING OPTICAL AND SCANNING ELECTRON MICROSCOPE:

A scanning electron microscope (SEM) is a type of electron microscope that produces images of a sample by scanning it with a focused beam of electrons. The electrons interact with atoms in the sample, producing various signals that can be detected and that contain information about the sample's surface topography and composition. The electron beam is generally scanned in a raster scan pattern, and the beam's position is combined with the detected signal to produce an image. SEM can achieve resolution better than 1 nanometer. The most common SEM mode is detection of secondary electrons emitted by atoms excited by the electron beam. The number of secondary electrons depends on the angle at which beam meets surface of specimen, i.e. on specimen topography. By scanning the sample and collecting the secondary electrons with a special detector, an image displaying the topography of the surface is created.

Polished samples were etched using beraha’s etchant

- CW00 etched in 100mL HCL + 50mL distilled water for 20 sec

- CW20 in 100mL HCL+ 50mL distilled water for 15sec

- CW40 in 50mL HCL+50mL distilled water for 20sec

- CW60 in 50mL HCL + 50mL distilled water for 15sec

1g of potassium metabisulphite purified (K2S2O5) and ammonium bifluoride (NH4HF2) were also added in the above solutions while preparing.

POTENTIOSTATIC TEST IN BERAHA’S SOLUTION:

Solution was prepared using 400mL distilled water + 70mL HCL+ 8g K2S2O5 +8g NH4HF2.The solution was deaerated using argon purging. The specimens were then held at their respective O.C.P for 8 seconds.

RESULTS AND DISCUSSIONS:

The microstructure of all the samples such as CW00, CW20, CW40, CW60 at 500X using optical microscope were given in fig.1.

THE MARTENSITIC TRANSFORMATION:

When deformed there is beginning of cell formation with dislocation tangles. When deformation increases equilibrium cell size with heavy dislocation density in cell walls formed; Because of the multiple interference of adjacent grains in a polycrystalline specimen multiple slip occurs readily and there is appreciable strain hardening.

DEFINITION OF COLD WORK:

Plastic deformation is carried out in a temperature region and over a time interval; such that the strain hardening is not relieved.

As deformation increases number of dislocation increases, which by virtue of their interaction results in a higher state of internal stress.

As received sample have 104-106 dislocation/mm2whereas after Cold working it varies between 1010-1012 dislocation/mm2.

In the early stages of plastic deformation slip is essentially on primary glide planes and the dislocation form coplanar arrays. As deformation proceeds cross slip takes place. The cold work structure forms high dislocation density regions or tangles, which further develop onto tangled network. Cold work is a cellular structure in which higher density dislocations tangles form the cell walls. The cell size decreases with strain at low deformation but soon reaches a fixed size, indicating that as strain precedes the dislocation sweep across the cells and join the tangle in the cell walls.

In polycrystalline metals, the crystallographic orientation of the grains differ with respect to the mechanical loading axis and thus of the active slip system vary from grain to grain. The dislocation slip and twin deformation are two competing modes and they often take place simultaneously to accommodate plastic deformation for FCC metals. Low stacking fault energy allows the occurrence of deformation twins in austenitic stainless steels at room temperature.

SFE=-53+6.2 wt %Ni+0.7 wt % Cr+3.2 wt % Mn+9.3 wt % Mo

But it is less pronounced at lower temperature and increase strain rate deformation and in materials with low SFE( stacking fault energy) because cross slip is difficult . As we know that SS304 has low SFE of 20mJ/m2 therefore the phenomenon is less pronounced.

Similarly to the formation of planar arrangements, twinning contributes to the strengthening of the material, acting as a kind of grain refinement, producing boundaries that serve as barrier to the movement of dislocations.

As seen from the microstructures the grains got elongated at higher strain which indicates that cold work produces elongation of grains in the principal direction of working. There is decrease in electrical conductivity due to an increased number of scattering centers. Also with increase in grain boundary,dislocation phase transformation and precipitation increases. Therefore there is higher martensite formation at higher deformation.

The fact that different slip systems can operate in adjacent regions of the same grain, results in complex lattice rotations which results in the formation of deformation bands. Since more slip systems are usually operative near the grain boundary, the hardness usually will be higher near the boundary than in the centre of a grain.

As the grain diameter is reduced more of the effects of gain boundary will be felt at the grain centre.

In the microstructure there will be slip bands or planes. The first sign of permanent deformation in a metal is the appearance of slip bands or lines. Slip bands are observed upon slightest deformations .as the degree of deformation is increased, the slip blocks in each separate crystallite turn to conform with the direction in which force acts and metal grains are elongated in that direction to form fibrous or banded structure.

% deformation= (F0-F1)/F1*100

Where, F0=cross section area of the test sample before deformation and

F1= cross section area of the test sample after deformation

CW00                                   CW20                                  CW40

CW60

Fig.1.Microstructure of CW00, CW20, CW40, CW60 at 500X using optical microscope

Martensite content:

Type 304 stainless steel is basically an austenitic stainless steel which is non-magnetic in nature but when the alloy is permanently deformed some of the austenite gets converted to martensite which has BCT structure and magnetic in nature so the cold worked SS304 shows magnetic character. As the amount of % deformation increases martensite formation increases and hence the magnetic nature increases, shown in fig.2.

Fig.2.MARTENSITE CONTENT vs. COLD WORK

With increase in cold work hardness also increases due to the formation of martensite in different systems of slip planes. In FCC crystal martensite forms in highly closed packed planes therefore it forms at {111} systems of planes. This martensite restricts the motion of dislocations and hence increases the hardness of the specimens.

Fig.3.HARDNESS vs. COLD WORK at low load          Fig.4.HARDNESS vs. COLD WORK at high load

(Creep-5s and dwell time-20s)                                      (Force-300gf and dwell time-15s)

Potentiodynamic Polarization Behaviour:

As the cold work increases passive current density (current density at 0.2V) also increases, that means corrosion resistance decreases, as illustrated in fig.

In all the curves from fig.3 a. to e. the passive film breaks at low current density for lower cold work and has high current density for higher cold work .This indicates that higher cold work materials are more prone to corrosion .The passive film form is  strong and cannot be broken easily. The O.C.P of cold worked materials almost remains same, hence O.C.P does not depend on cold work. The critical current density does not vary much for different cold worked specimens in S4 and S5 solution because they are less acidic and has less effect in corrosion.

The microstructure after polarization shows that there is patches formation near the grain boundaries because of the chromium depletion and also along the slip planes due to martensite transformation.We can see there is no intergranular corrosion or stress corrosion cracking.Corrosion test in H2SO4  and KSCN solution highly affects the slip plane. The cross slip are clearly visible in the corroded sample in the form of wavy lines.

For a particular sample in different solution we can see that critical current density increases as H+ concentration increases. The upper portion of the curve also state that current density increases for more acidic solution.

The passive current density does not depend on KSCN, therefore for S3 and S4 solution it is almost same in every samples. The passive current densityincreaseswith increase in H+ concentration of the solution increases.

The passive chromium rich oxide film on stainless steel surface protects it from corrosion. We can see the passive to trans-passive transition behavior .There is a formation of passive film of chromium rich oxide and current densities in the domain of passive potentials are very low. At high potentials, it enters the trans-passive state in which the current density begins to increase exponentially with the applied voltage. The main reason for increased current density at the onset of trans-passive for stainless steels is the conversion of Cr+3 to Cr+6 in the passive films itself. As potentials increase further in the trans-passive potential regime faster dissolution of chromium occurs at the oxide liquid interface leading to depletion of chromium throughout the oxide film.EPR test does not attack the grain matrix and the chromium carbide but dissolves the chromium depleted region and its immediately adjacent un-depleted region.

Fig. 3.(a).IN S1(1M  H2SO4, 0.01M KSCN) (b).IN S2(0.5M  H2SO4, 0.01M KSCN)

(c).IN S3(0.25M  H2SO4, 0.01M KSCN) (d).IN S4(0.25M  H2SO4, 0.005M KSCN)

(e).IN S5(0.1M  H2SO4, 0.001M KSCN)

Fig.5. Polarization curves in different solution.

OPEN CIRCUIT POTENTIAL (O.C.P)

| % Deformation | S1 | S2 | S3 | S4 | S5 |  |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | -0.433 | -0.448 | -0.454 | -0.462 | -0.465 |  |
| 20 | -0.468 | -0.481 | -0.462 | -0.461 | -0.471 |  |
| 40 | -0.457 | -0.449 | -0.465 | -0.479 | -0.471 |  |
| 60 | -0.432 | -0.450 | -0.461 | -0.480 | -0.465 |  |

Table-2

CURRENT DENSITY AT 0.2V (Passive current density)

| % Deformation | S1 | S2 | S3 | S4 | S5 |  |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 0.057 | 0.02 | 0.02 | 0.01 | 0.02 |  |
| 20 | 0.015 | 0.04 | 0.02 | 0.03 | 0.03 |  |
| 40 | 0.057 | 0.08 | 0.04 | 0.02 | 0.04 |  |
| 60 | 1.45 | 0.6 | 0.3 | 0.07 | 0.06 |  |

Table-3

Fig.6.Polarization curves of different cold work materials in different solution

CW00                       CW20                  CW40

CW60

Fig.7.Microstructure in S1 (1M H2SO4, 0.01M KSCN)at 500X

CW00                     CW20               CW40

CW60

Fig.8.Microstructure in S2 (0.5M H2SO4, 0.01M KSCN)at 500X

CW00                        CW20                        CW40

CW60

Fig.9.Microstructure in S3 (0.25M H2SO4, 0.01M KSCN)at 500X

CW00                    CW20                    CW40

CW60

Fig.10.Microstructure in S4 (0.25M H2SO4, 0.005M KSCN)at 500X

SEM IN BERAHA’S ETCHANT:

In CW00 we cannot see any martensite but as the cold work increases martensite also increases as seen from the images. The light portion were martensite .The sharp lines are slip lines/ bands. These lines are thin in CW20 but becomes thicker at CW40.The lines even turn out to be wavy at CW60 due to cross slip at higher cold work. Microstructure showing slip bands interactions,shear bands and martensite dislocations in moving slips interaction and it grows in number.

CW00                        CW00                         CW20

CW20                          CW40                      CW40

CW60                      CW60

Fig.10.Microstructure in Beraha’s etchant

CONCLUSIONS:

- The cold work structure forms high dislocation density regions or tangles, which further develop onto tangled network, therefore higher cold worked material has higher slip bands or planes

- As the amount of % deformation increases martensite formation increases and hence the magnetic nature increase

- When deformation increases equilibrium cell size with heavy dislocation density in cell walls formed; Because of the multiple interference of adjacent grains in a polycrystalline specimen multiple slip occurs readily and there is appreciable strain hardening.

- With increase in cold work hardness also increases due to the formation of martensite in different systems of slip planes

- As the cold work increases passive current density (current density at 0.2V) also increases, that means corrosion resistance decreases

- The passive film formed in higher cold work is weak and can be broken easily

- The critical current density does not vary much for different cold worked specimens in S4 and S5 solution because they are less acidic and has less effect in corrosion.

- There is no intergranular corrosion or stress corrosion cracking in

H2SO4 and KSCN solution. Corrosion test in H2SO4  and KSCN solution highly affects the slip plane. The cross slip are clearly visible in the corroded sample in the form of wavy lines.

- The passive current density does not depend on KSCN

- we can see that critical current density increases as H+ concentration increases

REFERENCES:

- Effect of composition and microstructure of austenitic stainless steel , paper in corrosion science section by V.Kain

- Corrosion science 43(2001)1519-1539 by C.Garcia,F.Martinetc

- Corrosion science 53(2011) 549-556 by FarzadMohammadin, JingliLuo

- Mechanical metallurgy ,third edition by George E.Dieter

- Corrosion Engineering by M.G.Fontana