PROJECT REPORT

Microstructural Characterization of

Gallium Nitride Thin Film Device Structures

Submitted by

V.S.S.Sri Lalitha

(12VV1A3126)

B.Tech III year

Department of Metallurgical Engineering

JNTU Kakinada-University College of Engineering Vizianagaram

Vizianagaram, Andhra Pradesh

Under the guidance of

Dr. D.V. Sridhara Rao

Scientist ‘F’

Defence Metallurgical Research Laboratory, DRDO

Ministry of Defence

Kanchanbagh Post, Hyderabad-500 058.

CERTIFICATE

This is to certify that the project work entitled “Microstructural characterization of GaN thin film device structures” is the bonafide work carried out by Ms.V.S.S.S.Lalitha, B.Tech III year, Department of Metallurgical Engineering, JNTUK-UCEV, Vizianagaram (Andhra Pradesh), under my supervision and guidance.

Dr. D. V. Sridhara Rao

Scientist ‘F’

Electron Microscopy Group

DMRL, DRDO

Hyderabad.

DECLARATION

This is to certify that this project report comprises of original work (except where indicated) carried out by me and due acknowledgements have been made in the text to all other material used.  The dissertation does not contain any classified information which will be detrimental to national security and has not been submitted in any form for another degree or diploma at any other institute/university.

(V.S.S.S.Lalitha)

B.Tech III year

Department of Metallurgical Engineering

JNTUK-UCEV, Vizianagaram, Andhra Pradesh

Countersigned by:

(Dr. D. V. Sridhara Rao)

Scientist ‘F’

Electron Microscopy Group

DMRL, DRDO

Hyderabad.

ACKNOWLEDGEMENT

I would like to express my sincere gratitude to Prof. P. Rama Rao, President, T R Anantharaman Education and Research Foundation for encouraging me towards research apart from academics.

I sincerely thank Dr G.Yesuratnam, Principal & Head, Department of Metallurgical Engineering, JNTUK-UCEV and Mr. G. Swami Naidu, Professor, Department of Metallurgical Engineering, JNTUK-UCEV for giving me an opportunity to do a project work at Defence Metallurgical Research Laboratory, Hyderabad.

I take this opportunity to convey my sincere thanks to Dr.Amol. A. Gokhale, Distinguished Scientist, Director, DMRL for granting permission to carry out the project work.

I am highly indebted to Dr. D.V. Sridhara Rao, Scientist ‘F’, Electron microscopy Group (EMG), DMRL for his guidance and support for successfully completing the project work. I am also thankful to the members of MBE growth (SSPL) and Director, SSPL for providing the GaN samples for characterisation studies.

I am also thankful to Dr.Partha Ghosal, Scientist ‘F’ (Group Head), Mr. Vajinder Singh, Sc.C, Mr. Deepak Kumar, Technical Officer and staff of Electron microscopy Group (EMG), DMRL for their timely cooperation and help in conducting the experiments and characterization studies.

I would like to thank Dr. Deepak Kumar Das, Sc.G & Group Head, HRD, DMRL and all the staff for their timely cooperation.

Some of the schematics of the experimental techniques are collected from internet sources.  Acknowledgements are due to these sources.

ABSTRACT

GaN is an important compound semiconductor.  It is widely used in thin film form in modern electronic devices such as HEMTs, LEDs and laser diodes.  GaN based thin films are grown on substrates by epitaxial growth methods.

This project work has focus on the investigation of the microstructure and composition of GaN HEMT device structures, consisting of multilayers, grown on sapphire substrates by plasma assisted molecular beam epitaxy. The experiments were conducted using advanced microscopic techniques, such as SEM, EBSD, TEM, EDS and AFM.  Observations were made on the chemical composition, surface morphology and misorientations of the grown III-nitride epitaxial films.  The studies showed the presence of threading dislocations and pits of different types at the surface. Also, the composition of the InAlN layer seems to be inhomogeneous. The films are single crystalline, predominantly in c-plane orientation and in epitaxy with the sapphire substrate.  The work is organized in different chapters describing introduction, experimental details, results & observations and summary.

Contents

| S.No. | Chapter | Page No. |
| --- | --- | --- |
| 1. | Introduction | 7 |
| 2. | Experimental details | 13 |
| 3. | Results and observations | 30 |
| 4. | Summary | 40 |
|  | References | 41 |

- Introduction

This chapter introduces the subject of Gallium Nitride and its important functional properties, device structures  and advanced microscopy techniques suitable for the microstructural and compositional characterisation of GaN based thin films.  Also, the objectives are listed.

1.1 : Gallium Nitride and its importance

The increase in the operating frequencies of telecommunications requires advanced electronic materials, such as III-Nitrides (Gallium Nitride, Aluminium Nitride, Indium Nitride and their ternary alloys) and the compatible substrates (viz., sapphire and silicon carbide).  Today, the transistor devices operating at microwave frequencies (in GHz range) are being possible only because of the advancements in the thin film growth techniques and the ability to grow heteroepitaxial structures of III-V semiconductors in nanoscale (or quantum well structures) with engineered compositional and bandgap profiles. In this context, Gallium Nitride (GaN) is an ideal candidate due to its superior functional properties (very high breakdown voltage, wide band gap, high-electron mobility, high saturation velocity and good Johnson’s figure of merit).  The nitrides have better functional properties vis-à-vis III-arsenides, hence they are more suitable for high-power, high-temperature and high frequency electronics. Also, they can be used to make photodetectors/photon sources for deep ultraviolet to infrared range, in particular high brightness white LEDs and blue laser diodes. Hence it is important to be aware of how these materials are grown into thin film device structures and to study the resultant microstructure and its effect on the functional properties.

Gallium Nitride is a wide band gap semiconductor (band gap 3.4 eV) and exhibits electron mobility of 440 sq.cm/volt/sec at 300K. It is hard, mechanically stable with high heat capacity and resists cracking in pure state. It is a non-flammable substance. The breakdown voltage of GaN is 600 V. It has a density of 6.15g/cc with melting point around 2500°C. It has hexagonal close-packed crystal structure with tetrahedral geometry (a=b=3.186Å, c=5.186Å) and with a thermal conductivity of 1.3W/cm/K.  The number of microstructural defects in GaN thin films per sq.cm is 108-1010, and they originate primarily due to the growth by heteroepitaxy.

Doping (addition of impurity atoms in p.p.m. concentrations) of a semiconductor introduces energy states within the band gap very close to the energy band edge, thus increasing the electrical conductivity of the material.  For example, the donar dopants form energy states close to the conduction band edge and contribute the electrons to the conduction band.   GaN crystal can be doped with silicon, oxygen and magnesium dopants. Silicon and oxygen doping gives an n-type semiconductor while magnesium doping gives a p-type semiconductor. However, due to the presence of silicon and magnesium, tensile stresses are induced, thus making the GaN film brittle.

GaN is used in making field effect transistors (FETs).   These unipolar transistors consists of a substrate wafer (sapphire, SiC etc) upon which the device quality epitaxial layers are grown, followed by Source, Gate and Drain metallisaiton.   The FETs act in the similar fashion as emitter, base and collector in a bipolar junction transistor (BJT). Source and Drain act as inlet and outlet respectively, for charge carriers, while the Gate modulates the channel conductivity. In recent years, GaN is being grown on silicon wafers, thus great scope and potential to replace the silicon-based metal oxide FETs, popularly called as MOSFETs.

The application of GaN for making high-electron mobility transistors (HEMTs) is an important field of research and required for military electronics, such as low-noise amplifiers (LNAs) with high power and high temperature operational capabilities and T/R modules used in the radar communications.  A typical HEMT structure consists of a buffer/AlN spacer (few nm thickness) /AlxGa1-xN (x=0.2-0.3, about 25 nm thickness) cap layer grown on a compatible substrate.  The buffer can be either GaN or AlN or a combination of both.  It is known that the initial growth conditions (growth temperatures, partial pressures of group III and group V atomic species etc) play an important role on the crystalline quality of the films.  In the conventional FETs, described above, the carrier mobility is significantly reduced due to the scattering of carriers by the ionised dopant impurities present in the channel at the operational frequencies.  This is addressed in the HEMT technology, in which the charge carriers (electrons) are transferred to the AlGaN/GaN interfacial region by the strong internal electric fields. These fields originate due to the polarisation effects (viz., GaN is polar along c-axis) and piezoelectric effects caused by heteroepitaxial growth of multilayers in the HEMT structure.  These electrons are confined to a very narrow region, behave as a two-dimensional electron gas (2DEG) due to quantum confinement effects and conduct at high mobility.  Hence, crystalline quality and the interfaces of epilayers are very important.

1.2 : Growth of Gallium Nitride based epitaxial thin film multilayers

The oriented growth of a crystalline material on the surface of another crystal is termed as epitaxy. In general, epitaxial growth is possible only if the lattice mismatch between the substrate and deposit is small. Epitaxial growth can be of the following ways:  (a) island (3D) growth, (b) Layer-by-layer (2D) growth and (c) Stranski-Krastanov (S-K) growth in which the 3D islands grow on a 2D wetting layer (example : quantum dots). The island growth occurs when the deposit atoms are strongly bound among themselves than with the substrate; small clusters are nucleated on the substrate and grow into islands. These islands grow into a continuous film. The layer-by-layer growth arises when the deposited atoms are strongly attracted to substrate than to themselves and form a single layer over the substrate. Additional material deposition gives multilayered epitaxial growth. The epitaxial growth may give rise to either textured orientation or azimuthal orientation (textured, if the orientation of substrate and deposit is same; azimuthal, if the orientation of substrate differs with that of the deposited film).

GaN based thin film multilayers can be synthesized by physical vapor deposition (PVD) or by chemical vapor deposition (CVD) methods, under suitable vacuum conditions. PVD methods include heating, sputtering, electron beam evaporation and LASER beam evaporation. The deposition of thin film takes place by adsorption of the vaporized species on the surface of the substrate, followed by nucleation and growth.  Molecular beam epitaxy (MBE) and its variants (Nitrogen plasma MBE or PAMBE, ammonia MBE etc) are some popular PVD methods.  In this method, a thin film of gallium nitride is grown by depositing gallium and atomic nitrogen species over substrate under ultra-high vacuum conditions. The growth parameters are chosen in such a way that Ga and N species diffuse over the surface of substrate, combine and form stoichiometric continuous film through nucleation and growth mechanisms.  This technique offers the growth of epitaxial films with abrupt interfaces with compositional profiles.  In the present work, PAMBE technique was used for the growth of AlGaN/GaN and InAlN/GaN HEMT structures.

In CVD, the thin film is formed by the chemical reactions of source gases (ammonia and organometallics such as trimethyl gallium) at elevated temperatures on the surface of the substrate. Organo-metallic chemical vapor deposition (MOCVD) is one of the widely used CVD methods. This method offers relatively higher growth rates vis-à-vis MBE, hence widely used by the industry for commercial applications.

1.3 : Gallium Nitride & Microstructrual Defects

It is highly desirable to grow defect-free thin films of III-Nitrides.  In this context, the GaN crystalline quality is influenced by the heteroepitaxy growth processes.  The GaN bulk substrates are too expensive and available only in small sizes. Hence, GaN is widely grown on foreign substrates such as sapphire, silicon carbide and (111) silicon.  Due to the lattice mismatch [about 16% for GaN-sapphire, 3.5% for GaN-SiC and -17% for GaN-Si systems] and thermal mismatch [about -35% for GaN-sapphire, 25% for GaN-SiC and 54% for GaN-Si systems] between the GaN film and substrate, various microstructural defects - point defects, dislocations, stacking faults, v-pits and micro pipes can be formed.  Also, the GaN films exhibit mosaicity (i.e., the initial growth of GaN film is in the form of small crystallites with twist and tilt misorientations, which undergo coalescence during the later stages of growth thereby forming a continuous film).  Dislocations are the line defects, which are known to degrade the functional properties; hence their formation should be minimised.  The perfect dislocations are edge, screw and mixed-type.  In an edge dislocation, the Burgers vector is always perpendicular to the dislocation line while it is parallel to the dislocation line in a screw dislocation.   Transmission electron microscopy (TEM) is widely used to observe the dislocations, stacking faults and v-pits.  Stacking fault is an interruption in the stacking sequence of lattice planes of the crystal. It can be formed in basal planes and prismatic planes.   Micropipes are empty core-screw dislocations with large strain energy, usually present in single crystal SiC substrates. The micropipes can propagate from the SiC substrate to the overgrown epitaxial layers.  V-pits take their origin from the vertex of threading dislocations to the stacking mismatch boundaries. These are induced by stacking faults and island growth due to large lattice mismatch.

1.4 : Advanced Microscopy Techniques:

The microscopy techniques are ideally suited to study the above microstructural defects.  Scanning electron microscopy (SEM) is suitable to study the surface morphology.  Atomic force microscopy (AFM) can be used for the quantitative surface roughness studies.  Electron-backscattered diffraction (EBSD) technique is useful to investigate the mosaicity of the GaN films.  Energy-dispersive x-ray spectroscopy (EDS) technique offers the chemical compositional information. Cross-sectional TEM reveals the individual epitaxial layers in the multilayer structures and the microstructural defects.  The TEM based electron diffraction technique is useful to study the orientation relationships between GaN and substrate and also the epitaxy of different layers in the HEMT structure.

1.5: Objectives of the project

The primary objectives of this project are as follows:

(a) To get familiarisation with the advanced microscopy techniques (optical microscopy, SEM, EBSD, AFM, TEM and EDS) for microstructural and compositional studies,

(b) To get introduced to the crystallography softwares for creating the crystals, simulation of electron diffraction patterns and EBSD patterns,

(c) To learn specimen preparation methods for SEM and TEM, and

(d) To apply the above techniques/methods for the studies of GaN HEMT device structures.

2. Experimental Details

This chapter describes the details of growth of GaN HEMT device structures and characterisation techniques employed for the microstructural and compositional studies.

2.1: Growth of GaN HEMT device structures

The deposition of GaN HEMT device structures on c-plane sapphire substrate was performed in a plasma-assisted molecular beam epitaxial (PAMBE, SemiTeq-make) system under ultra-high vacuum (UHV) conditions.  The substrates were loaded in the growth chamber as per the standard procedure.  Ga, In and Al sources in the effusion cells were heated and their evaporation was controlled through the individual shutters to the cells.  Due to the UHV conditions, the mean free path of the vaporized atomic species is very large.  Initially, the Gallium source was heated to sublimate gallium. Then, nitrogen plasma was injected into the ultra-high vacuum growth chamber. Nucleation and growth of the GaN film on the surface of the substrate was monitored by in-situ RHEED (Reflection High Energy Electron Diffraction) technique.  The RHEED patterns were used to study the surface reconstruction behavior, growth mode and the deposition thickness in terms of monolayers.  Subsequently, AlN spacer layer (about 1-2 nm thickness) and either AlxGa1-xN or InxAl1-xN layers were grown.

Two types of HEMT structures were grown, by varying the cap layer’s composition, as follows:

(a) sample-1: (0001) sapphire substrate/ buffer / AlN spacer / AlxGa1-xN cap

(b) sample-2: (0001) sapphire substrate/ buffer / AlN spacer / InxAl1-xN cap

The microstructures of the above structures were investigated and the results are presented in this report.

2.2 Characterisation Techniques:

In this project, various microscopy techniques were used for the microstructural and compositional characterization, viz., optical microscopy, SEM, EBSD, TEM, EDS and AFM.  In this section, the working principles of the equipments are briefly described along with the relevant experimental details.

2.2.1 Optical Microscope

The optical microscope (light microscope) is useful to study the surface morphology of the samples.  The schematic (Fig. 2.1) shows various components of the microscope: eye piece, objective lens, light source, a semi-silvered glass and a condenser lens. The light from the light source gets reflected by a semi-silvered glass kept at 45o tilt, passes through the objective and then on to the sample surface. It is reflected back by the sample and is partly transmitted through the glass to the eye piece. Thus, the microscope produces the image of the surface by reflection of light. The microstructure/ features of the surface can be viewed under various magnifications viz., 50X, 100X, 200X and 500X. In the present studies, Leika-make optical microscope (Fig. 2.2) was used for the inspection of the surface of SEM and TEM specimens at various stages of sample preparation.

Fig.2.1 : Line diagram of a light microscope

Fig. 2.2 Optical microscope (Leica-make)

2.2.2 Scanning Electron Microscope (SEM)

In a SEM, as the name suggests, an electron beam raster scans the surface of the specimen.   Due to the interaction of the incident electron beam and specimen, several events occur viz., backscattered electrons (BSE), secondary electrons (SE) and emission of characteristic x-rays. The BSE images reveal the phases due to z-contrast, whereas the SE images show the surface features. Due to employment of short wavelengths (electrons), the depth of field and depth of focus are much greater with electron microscope vis-à-vis optical microscope.  These are the desirable features.  The typical maximum magnification and spatial resolution achievable by FEG SEM are of the order of 5,00,000x and 1 nm respectively.

The working principle of SEM is shown schematically in Fig. 2.3.  The electron beam emitted from the source (tungsten or LaB6 filament by either thermionic emission or field emission) interacts with the specimen after passing through Wehnelt cylinder, anode, electromagnetic lenses (condenser and objective lenses) and scan coils.  The condenser lens controls the number of electrons in the beam with respect to objective aperture size.  The objective lens focuses electrons onto the sample surface. Objective aperture controls the number of electrons reaching the sample surface. Larger is the aperture size; smaller is the depth of field. The strength of the objective lens is inversely proportional to the working distance from the sample (probe diameter on the sample). Maximum spatial resolution is obtained with short working distances i.e. with less diameter of probe on the sample surface. Scan coil present above the objective lens controls the position of electron beam on the sample surface. Scan coils are of the types- continuously moving and discrete moving. Continuously moving coils contribute to analogue scan whereas discrete moving coils dwell over a particular point before moving to next point thus contributes to digital scan. Current given to X-scan coils move electron beam in X-direction and is termed as horizontal scan. Similarly, Current given to Y-scan coils move electron beam in Y-direction and is termed as vertical scan.

Fig.2.3. Working principle of SEM

In the present studies, FEG SEM (Fig. 2.4) is used for the investigation of the surface features.  The samples were ultrasonically cleaned in acetone for 5 minutes, followed by isopropyl alcohol (IPA) cleaning for 5 minutes and then dried under IR lamp so that the surface is clean prior to loading into the SEM’s specimen chamber.

Fig.2.4 : SEM-EBSD-EDS system in DMRL

2.2.3 Electron back-scatter diffraction

EBSD is one of the SEM based advanced techniques, useful for the quantitative crystallographic misorientation studies. EBSD patterns were first observed by Kikuchi (1928) in Transmission Electron Microscope (TEM). Von Borsch (1937) extended Kikuchi’s work.

A typical SEM used for the EBSD studies consists of an electron gun, an EBSD detector, a CCD camera and a specimen chamber.   The prepared sample is mounted on the sample holder and is appropriately fixed to the stage/platform at an angle of 70o to the vertical (i.e., incident electron beam direction) for greater interaction volume of electron beam and the sample than when held horizontally.  This geometry is shown in Fig. 2.5. A beam of electrons from the electron gun is focused onto the sample and raster scans the surface emitting high energy back scattered electrons along with secondary electrons and X-rays. The backscattered electrons satisfying the Bragg’s condition form Kossel cones which when imposed on the phosphor screen produce Kikuchi diffraction pattern (Fig.2.6).

In the present studies, Zeiss-make SEM with FEG source and fitted with Oxford-make EBSD detector was used for the investigations of crystalline misorientations of the films.

Fig.2.5: Geometry of Sample and EBSD detector inside the SEM.

Fig.2.6:  EBSD pattern formation

2.2.4 Transmission Electron Microscope (TEM)

TEM is an advanced electron optics instrument, in which the incident electron beam transmits through the electron transparent specimen and provides the details of the microstructure, crystallography and composition with very high spatial resolution.  A typical TEM consists of an electron gun from which electron beam is emitted, which is subsequently accelerated to high energy (of the order of 200 kV) and passed through a series lenses and apertures. The incident electron interacts with the specimen and its amplitude/phase undergoes changes.  These changes are recorded in the form of bright field (BF) & dark field (DF) images and lattice images.  Due to the short wavelength of the electrons (comparable to the lattice spacings of the sample), diffraction of electrons occurs.  This information appears as electron diffraction pattern, which is useful to study the crystallography of phases present in the specimen.  The modern TEM is connected with energy dispersive x-ray spectroscopic (EDS) detector as an accessory, which is useful for chemical compositional studies.

Fig.2.7: FEI-make Tecnai G2 (200 keV) TEM with EDS detector, DMRL

It is to be noted that electron transparent specimens are required for the TEM investigations.  In this regard, the TEM specimen preparation is a major limitation.  Also, the semiconducting materials are brittle; hence the samples are prone to breakings during mechanical lapping and polishing.  Hence, the preparation TEM specimen is highly time consuming with low yield.

2.2.5 Energy Dispersive X-ray Spectroscopy

Each element has unique atomic structure.  Hence, due to the interaction with energetic electrons, characteristic x-rays are emitted by the atoms of the specimen.  These x-ray photons are detected by the EDS detector.  It has a lithium drifted silicon detector and associated electronics for measuring the x-ray counts as a function of energy of x-ray photons.  The analysis of EDS X-ray spectrum (x-ray counts versus energy of x-ray photons) helps in the quantitative compositional studies of different elements in the samples.

In the present studies, compositional studies were performed by using the EDS detectors connected to Zeiss-make SEM (FEG source) and FEI-make Tecnai 20 G2 TEM.

2.2.6 Atomic Force Microscope (AFM)

AFM facilitates the study of the topography of the sample surface and helps in better understanding of the presence of v-pits, micro pipes etc.  It can sense the atoms on the surface by raster scanning the surface and measuring the repulsive forces between the tip of the probe and the sample. The tip rests on cantilever probe. The variation in the height of cantilever probe from the surface influences the force acting on the probe and therefore deflection of the probe takes place. Basing on the tip deflection information, an image of the observed surface can be created. Thus, AFM helps in recording the topographical map of the sample surface.

Fig.2.8: Principle of AFM

In AFM, a sharp tip (µm sized) at the end of the cantilever of the probe is used to detect the forces (attractive and repulsive as well) and produce high resolution images. The vertical and lateral deflections of the cantilever are measured by using an optical lever. The optical lever operates by reflecting a laser beam off the cantilever. The reflected laser beam strikes a position-sensitive photo-detector consisting of four-segment photo-detector. The differences between the segments of photo-detector of signals indicate the position of the laser spot on the detector. The movement of the tip is around ± 20 nm vertically. The topography obtained from AFM depends upon the size, shape and functionality of the tip of the probe.

Fig. 2.9: Tip of the probe in AFM (courtesy: internet source)

Depending on the sample-tip interactions, AFM can be operated in either contact mode or non-contact mode.  The contact mode can be either constant force type or constant height type.  In the former, a feedback loop is used to move the tip up and down and keep its deflection constant.  Whenever there is a change in force due to change in distance of the tip from the sample, the voltage is balanced to the prior set force point (also called feedback set point) to nullify the changes in the force. The deviations from the original force-distance curve are termed as errors. The changes in either voltage or amplitude are plotted. In this way, the changes in the voltage are monitored to give the topography of the surface.  In the constant height type, the cantilever deflection is measured directly and the deflection force on the tip is used to calculate the distance from the surface. Since no feedback loop is required for this type of measurement, it is appropriate for quick scans of samples with small height differences.  In non-contact mode the tip doesn’t touch the sample. It just oscillates very close to the surface (at a distance of approximately 5-10 nm).  A major advantage of this mode is negligible friction forces, making this mode capable for measurements of biological and polymeric samples without destroying the surface.

Fig.2.10: AFM Probe-surface interactions: Contact and non-contact modes

Force-distance curves give information about the attractive and repulsive forces acting on the probe tip. The repulsive forces acting on the tip are the electrostatic forces of repulsion (like charges repel each other) due to the presence of electrons in both the tip and the sample whereas; the attractive forces are due to the Vander Waal’s forces of attraction.

Fig.2.11: Force-distance curve in AFM

2.3 Crystallography softwares

2.3.1 Crystal maker:

Crystal maker software is useful for creation of crystals and indexing of the electron diffraction patterns. It enables the visualisation of the unit cell and atom positions.  Also, the stereographic projections of lattice planes and directions along the different orientations of the crystal can be plotted as per the user requirements.  In this work, this software was used for the creation of unit cell of GaN (Fig. 2.12a), simulation of electron diffraction patterns (Fig. 2.12b is a representative pattern) and the experimental patterns were analysed with the help of these simulations.

Fig.2.12: (a) GaN crystal along [11-20] orientation; (b) simulated electron diffraction pattern and (c) corresponding stereographic projection of GaN crystal.

2.3.2  Espirit DynamicS (EBSD software):

ESPIRIT DynamicS software (commercially available from M/s Bruker) is suitable for the simulation of EBSD patterns under a variety of conditions including the incorporation of dynamical effects.  The number of atoms, unit cell, crystal symmetry, lattice parameters, Euler angles and pattern-centered values can be incorporated for a desired EBSD pattern.  Using this software, EBSD pattern of GaN crystal was simulated and our experimental patterns were loaded and matched by auto-correlation. For example, the EBSD simulated patterns for GaN crystal under kinematical (Fig.2.13 a) and dynamical diffraction conditions (Fig.2.13b) are shown.  The experimental pattern (Fig. 2.13c) is matched with the simulated pattern through auto-correlation (Fig.2.13b).  Thus, this software is useful for the analysis of EBSD patterns.

Fig.2.13: EBSD patterns of GaN near <0001> orientation: simulated patterns (a) kinematical conditions and (b) dynamical conditions.  The experimental pattern is shown in (c).   The GaN crystal considered for the simulations is shown in (d).

2.4 Electron Microscopy specimen preparation

2.4.1 SEM/EBSD/AFM

The sample preparation for SEM includes cleaning the surface of the sample using acetone in ultrasonic cleaning equipment for 5 minutes, in order to remove the dust and greasy contamination.  This was followed by cleaning in isopropyl alcohol under ultrasonication for 5 minutes.  Then, the samples were dried under IR lamp prior to the loading for microscopy investigations.

2.4.2 Cross-sectional TEM specimens

For TEM analysis, the sample must be 3mm in diameter and electron transparent in thickness (~100 nm). In the present work, cross-sectional TEM samples were prepared by following the steps given below:

- Slicing and grinding of the sapphire wafer on which a thin film of GaN is grown. Slicing was done by using a Buehler-make isomet low-speed saw (Fig. 2.14).

Fig.2.14. BUEHLER ISOMET low speed saw

- Preparation of a sandwich structure, by gluing of two slices of samples such that both the shiny surfaces (GaN epilayers) are facing together. For bonding, Devcon 5-minute epoxy was used.  Tweezers were used to apply small pressure on the glued sandwich to aid in proper sticking.  Here it is noteworthy to remember that too much stress with tweezers results in crack formation.

Fig. 2.15 Cross-sectional TEM sample viewed under an optical microscope.

- The glued sandwich was inserted into a slotted brass tube (inner diameter : 2 mm) provided with a brass cap (outer diameter : 3 mm). Then, it was cut into 500 micron thick slices using the low speed saw.

- One of the slices containing the sandwich was glued onto a copper grid of 3mm diameter so as to achieve final sample diameter for TEM analysis.

- The sample was well ground and polished by fixing in a Gatan-make disc grinder, using emery papers with grit nos. 320, 600, 1200 and 2500.

- The sample, at various stages of lapping and polishing, was observed for a well-polished surface under an optical microscope.  Thus, the disc thickness was brought down to below 40 microns (Fig. 2.15).

- Later, argon ion beam thinning was done by precision ion polishing system (PIPS) at 5 keV with ion beam modulation, to realize a small hole at the center of the sandwich structure.  The edges of this hole were found to be electron transparent.  These regions were studied.

3. Results & Observations

This chapter describes the results: surface morphology, chemical composition, epitaxy, defects and mosaicity.

The surface of sample-1, as revealed by the plan-view SEM images, is smooth (Fig. 3.1a).  In this case, very small pits are observed throughout the surface, which could be formed due to the termination of the threading dislocations (TDs) at the surface.  However, the sample-2 has a rough surface with relatively coarse-sized shallow pits (Fig.3.1b).   These pits were examined at higher magnification with (Fig. 3.2a) and without (Fig. 3.2b) specimen tilting.

Fig.3.1 SEM images of samples-1 (Fig. a) and 2 (Fig.b) at a magnification of 15000X

Fig. 3.2 : SEM images showing different types of pits.  Fig. (a) shows the surface at 70˚ specimen tilt and Fig.(b) represents the plan-view image without specimen tilt.

These images clearly showed the presence of four-types of pits: (1) coarse-sized (200-300 nm in diameter) pits with an areal density of the order of 3 per m2, (2) smaller pits (size is of the order of 10 nm) with an areal density of the order of 40 per m2, (3) arrays of smaller pits, and (4) isolated pits in the coarse shallow pits.  The areal density of the smaller pits (in the range of 109 per cm2) is close to the expected density of threading dislocations (TDs), hence it is likely that these pits correspond to the TDs, which are terminated at the surface.   To examine these surface features quantitatively, AFM investigations were conducted and the results are displayed as Fig. 3.3.  Fig. 3.3(a) shows the coarse pits (X, Y) in three-dimensional (3D) view.  The analysis of the pit X (Fig.3.3b) shows that this pit has a diameter of about 250 nm and a depth of about 7 nm, whereas the pit inside this shallow pit has a depth of about 12 nm (Fig. 3.3c).  The individual pit (Fig. 3.3d) has a depth of about 10 nm.

SEM based semi-quantitative standardless EDS analysis (Fig. 3.4a, 3.4b) showed that the coarse sized shallow pit has relatively lean indium content (32 wt.%) vis-à-vis adjacent regions (37.2 wt.%) free from such pits.  This analysis is done by assuming that the sum of the contents of In & Al elements = 100 wt.%.

The above results suggest that the InxAl1-xN cap layer has compositional inhomogeneity.  Also, the appearance of coarse shallow pits with relatively lean-indium content indicates the possibility of desorption losses of indium from this layer.  It is known that the element Al has relatively higher sticking coefficient; also indium has the tendency of surface segregation.  These two mechanisms may be lead to the formation of these coarse-sized shallow pits.

A study was performed to assess the effect of operating voltage of SEM on the imaging of pits at the surface.  The voltage was varied from 2 kV to 20 kV.  It is known that the specimen’s volume excited by the electron beam is a dependent on the kV; a relatively lower kV is expected to reveal the surface features more clearly.   This aspect can be qualitatively seen in these images.  Also, the images (Fig. 3.5) suggest that an operating voltage of 5 kV may be a good option for the visualization of the surface features with good contrast.

Fig. 3.3 : AFM results: (a) 3D-view of the surface morphology, (2) 2D-projection of the surface morphology, (c) line scan LM across the coarse pit “X” and (d) line scan NO across an isolated pit.

Fig.3.4 (a) SEM image showing the regions from which EDS analysis was performed.  Fig.(b) EDS spectrum-1 and (c) EDS spectrum-2 (both spectra at 15kV) indicating indium content of 32% and 37.2% by weight.  The most intense peak (not labeled) corresponds to Ga element and it was not considered for this semi-quantitative analysis.

Fig. 3.5 : SEM images showing different types of pits at different operating voltages of SEM.

It is known that GaN based films grown on sapphire substrates exhibit mosacity.  Hence, EBSD studies were performed to analyse the crystalline misorientations of the film.  The results (Fig. 3.6, 3.7) show that the film is highly textured with basal planes of the film parallel to the growth surface.

A cross-sectional TEM study of sample-1 was performed.  The results are shown in Fig. 3.8.  The studies resolved the thin AlN spacer layer (Fig.3.8b) and the combined selected area diffraction pattern (SADP) from the GaN-sapphire regions showed that the GaN film is epitaxial with respect to the underlying sapphire substrate.   The SADP of GaN film is shown in Fig.3.9 (a) and analysed with the help of crystal maker software (Fig. 3.9b).  The dark field TEM image (Fig. 3.8d) clearly revealed the threading dislocations propagating across the GaN epilayer.  These dislocations are originated at the GaN-sapphire interface.

The composition of GaN film is also studied by the EDS technique.  The studies showed that GaN is highly pure and has no noticeable out-diffusion of Al from sapphire (Fig. 3.10).

Fig. 3.6 : EBSD results showing: (a) crystal orientation map, (b) band contrast map, (c) and IPZ map.  The color-coding is shown in (d).

3.7 : Pole figure sheet showing the crystalline mosaicity projected along different axes.

Fig. 3.8. TEM results-(a) Bright field TEM image showing the cross-section of GaN HEMT structure.  (b) The top region (shown with white arrow in Fig.a) is shown at a higher magnification, resolving the AlGaN/AlN HEMT layers;  (c) The combined selected area diffraction pattern (SADP) corresponding to GaN and sapphire. (d)The analysis of SAD pattern of GaN- the dark field image showing dislocations in GaN film, which were originated at the interface and threading throughout the film.

Fig. 3.9:  Selected area diffraction (SAD) pattern of GaN film along <10-10> orientation. (a) Experimental pattern, (b) SAD pattern simulated by Crystal maker software.

Fig.3.10: Energy dispersive x-ray spectroscopy (EDS) studies of Sapphire and GaN regions.

4. Summary

This project work had focus on introducing the advanced microscopy techniques (optical microscopy, SEM, EBSD, AFM, TEM and EDS), crystallography softwares, electron microscopy specimen preparation methods and their application for the microstructural studies GaN thin films.  The following is the summary:

(1) GaN HEMT structures were grown on sapphire by plasma assisted molecular beam epitaxy, with AlGaN (sample-1) and InAlN (sample-2) cap layers respectively.

(2) SEM & AFM studies of sample 2 showed the different types of pits at the surface:  coarse-sized shallow pits, relatively smaller pits, arrays of smaller pits and isolated pits inside the coarse shallow pits. The semi-quantitative EDS studies suggested that the coarse pits are indium-lean.  Sample 1 had a relatively smooth surface with small pits, which are barely seen at low-magnificaiton.  The density of these pits can be related to the threading dislocation density.

(3) Electron backscattered diffraction studies is very effective in determining the crystalline mosaicity.  The grown films are highly textured with basal planes parallel to the growth surface.

(4) From the detailed SEM secondary electron imaging studies, it is qualitatively evident that the operating voltage and specimen tilt are two important experimental parameters for visualization of the surface features such as pits.  This is due to the reason that the interaction volume of the specimen and spatial resolution of SEM are related to them.

(5) Cross-sectional TEM microstructural studies aided in understanding the epitaxial multilayers grown over the sapphire substrate.  Also the presence of threading dislocations is observed.

The findings of this work are at a preliminary level, primarily due to short-term project, hence more scope for further investigations, such as detailed compositional studies of InAlN layer, possible presence of indium-rich clusters in InAlN film, threading dislocations, interfaces etc .

References

- https://en.wikipedia.org/wiki/

- Principles of physical vapor deposition of thin films by K.S.SreeHarsha

- Introduction to electron microscopy by Saul Wischnitzer- Pergamon press.

- Transmission electron microscopy and diffractometry of materials by Brent Fultz & James Howe- Springer publications.

- Scanning electron microscopy and X-ray analysis by Goldstein, J.I – plenum press.

- Advances in optical and electron microscopy by Baver.R and Cosslett.V.E.

- A guide to the principles and techniques of AFM and other SPM methods

- A Guide to AFM Image Artifacts (Pacific Nanotechnology)

- Atomic Force Microscopy (nanoHUB.org)] – a presentation/podcast introducing AFM

- http://www.matter.org.uk/tem/

- http://www.doitpoms.ac.uk/tlplib/tem/links.php

- http://www.doitpoms.ac.uk/tlplib/afm/index.php

- Texture and Anisotropy – Preferred orientations in polycrystals and their effect on materials properties by U.F Kocks, C.N Tomé and H.-R Wenk, Cambridge University Press, Cambridge 1998

- Crystallography and Crystal Defects, 2nd edition, A. Kelly and K.M. Knowles, John Wiley and Sons, Chichester, 2012

- A. Putnis, Introduction to Mineral Sciences, Cambridge University Press, 1992

- C. Hammond, The Basics of Crystallography and Crystallography, III Ed, Oxford University Press, 2009

- B.D  Cullity, S.R Stock, Elements of X-Ray Diffraction, Prentice Hall, 2001

- International Tables for Crystallography http://it.iucr.org/A/

- J.S. Blakemore, Solid State Physics, Cambridge University Press, 1985.

- http://doitpoms.ac.uk/tlplib/Optical Microscopy and Specimen Preparation/index.php

- http://www.howstuffworks.com/laser.htm