SYNTHESIS AND CHARACTERIZATION OF Cu-Cr-CNT                                                                        COMPOSITE

By

Zulkifl Hussain Rabbani

Bachelor of Technology

IN

DEPARTMENT OF METALLURGICAL AND MATERIALS ENGINEERING

NATIONAL INSTITUTE OF TECHNOLOGY

SRINAGAR (J&K)

UNDER THE GUIDANCE OF

Dr. TATA N RAO, SCIENTIST-G

SHRI S.B. CHANDRASEKHAR, SCIENTIST-E

Mr. P.V.V. SRINIVAS, TECHNICAL OFFICER

CENTRE FOR NANO MATERIALS

International Advanced Research Centre for Powder Metallurgy

& New Materials (ARCI)

INTERNATIONAL ADVANCED RESEARCH CENTRE FOR POWDER                               METALLURGY AND NEW MATERIALS (ARCI),

HYDERABAD

CERTIFICATE

This is to certify that the work entitled “Cu–Cr–CNT Composites – Synthesis and Characterization” is a bonafide work carried out by Ms Zulkifl Hussain Rabbani in partial fulfilment of the requirements for the award of the degree of Bachelor of Technology in Dept. of Materials and Metallurgical Engineering, National Institute of Technology, Srinagar, Jammu& Kashmir. The results embedded in this report have been verified and found satisfactory.

Forwarded by-

P.V.V. Srinivas

Technical officer-A

Centre for Nano Materials

ARCI, Hyderabad.

Project Guide:                                                                               Team Leader:

Shri S.B. Chandrasekhar, Scientist-E                                    Dr T.N. Rao, Scientist-G

Centre for Nano Materials,                                                              Centre for Nano Materials,

ARCI - Hyderabad			 				ARCI - Hyderabad.

List of contents                                                                    Page No.

Acknowledgement--------------------------------------------------------------- 5

Abstract ---------------------------------------------------------------------------- 6

Chapter 01

- Introduction ---------------------------------------------------------------- 7

  - Raw Material Required ------------------------------------------ 9

  - Mechanical milling ----------------------------------------------- 11

  - Consolidation of Powder --------------------------------------- 14

  - Vacuum furnace ------------------------------------------------- 16

Chapter 02

2.0 Characterization

2.1 Optical Microscope ----------------------------------------------- 23

2.2 Vickers Hardness Indenter -------------------------------------- 24

2.3 Scanning Electron Microscope --------------------------------- 26

2.4 Electrical conductivity measurement ------------------------ 29

Chapter 03

- Experimental procedure

  - Synthesis of Cu-Cr-CNT nanocomposite powder ------------- 30

  - Reduction of nanocomposite powder --------------------------- 30

  - Sintering of powder -------------------------------------------------- 31

  - Solutionizing  treatment--------------------------------------------- 31

  - Ageing -------------------------------------------------------------------  33

  - Conductivity measurement ----------------------------------------  33

  - Metallographic specimen preparation --------------------------  33

  - Microhardness measurement -------------------------------------  35

  - SEM Characterization ------------------------------------------------  35

Chapter 04

- Results

4.1 Electrical conductivity ------------------------------------------------- 36

4.2 Microhardness ---------------------------------------------------------- 37

4.3 Microstructural analysis ---------------------------------------------- 39

Chapter 05

- Discussions ---------------------------------------------------------------------- 41

Chapter 06

- Conclusions --------------------------------------------------------------------- 42

References ----------------------------------------------------------------------------- 43

ACKNOWLEDGEMENT

I am extremely thankful to Dr. G Sundararajan, Director, ARCI and Dr. Srikant V Joshi, Associate Director, ARCI and Dr.T.N. Rao, Team Leader, Centre for nanomaterials for providing me an opportunity to carry out my summer training at ARCI, Hyderabad.

It is my great pleasure to express my deep sense of gratitude to my research supervisor Mr. P.V.V. SRINIVAS,TECHNICAL OFFICER “A” for his keen attention and inspiring guidance and for spending precious time from his busy schedule to provide encouragement and full support during my training period at ARCI.

I am extremely thankful to S.B CHANDRASEKHAR, SCIENTIST “E”, center for nano materials for his guidance.

My gratitude to all the Scientists and Technical Officers, involved for the support and help in characterization part and obtaining the results at the right time, especially Mr. Govind Kumar.

I would also like to share my heartfelt gratefulness for Mrs. Nagini, SRF and Mr. Sai Karthik for their help during the metallographic sample preparation.

I am grateful especially to Dr. T.N. Rao and all the colleagues in ARCI for providing me with such a helpful, friendly and caring atmosphere. I am obliged to each one of them. Their constant support has been inductive of my perseverance. The dedication and sincerity shown by JRFs, SRFs and Scientists working in ARCI, Hyderabad has been a source of inspiration for my work. Throughout the internship period the faith of my instructors and guides in me has been instrumental in my empowerment. I am appreciative of all the favors done to me and for the provision of everything required.

I would finally, not forget to mention how obliged I am, to my parents who have been ever supportive and guided me at each step of my life. It is solely because of their trust in my abilities and faith in me that I have managed to reach this far. Without their support this could simply not be possible. I shall prove to be a confidant.

ABSTRACT

The experiment was carried out using a composite powder of copper (Cu), chromium (Cr) and carbon nano tubes (CNT) with the composition being 1wt% Cr and 0.5wt% CNT, mechanically alloyed in high energy mill or planetary mill. The powder sample was then reduced in a vacuum furnace in hydrogen atmosphere at 600 0C. The reduced powder was consolidated by spark plasma sintering (SPS) technique, which produced a sintered sample of about 93%-95% of its theoretical density. The sample was then sent for heat treatment processing at a temperature of 900 0C. Following annealing, the samples underwent ageing at two different temperatures 400 0C and 600 0C. Different heat treatment processes were carried out in order to improve upon the hardness of the composite. The samples revealed promising values of hardness but with some compromise in their conductivity values.

The heat treatment processes were followed by characterization by electrical conductivity, Vickers micro hardness and scanning electron microscopy (SEM). The tests revealed a reduction in conductivity of annealed sample, but further heat treatment (ageing) showed an improvement in the conductivity values.

Symbols used:

- Pa – Pascal, W – Watt, m – meter, h – hour, t – ton, kg – kilogram, V – Volts, Hz – Hertz.

- S – Siemens, nm – nanometer, M – mega, T – tera, G – giga, K – Kelvin, mbar – millibar.

- Pa, mbar, kgf, mmHg – units of pressure.

- W/m-k – unit for thermal conductivity.

- MS/m – unit of electrical conductivity.

CHAPTER 01

- INTRODUCTION

Many of our modern technologies require materials with unusual combination of properties that cannot be met by the conventional metal alloys, ceramics and polymeric materials. This is especially true for materials that are required for aerospace, underwater and transport applications. For example in aircrafts, we require materials that are low in densities, are strong, stiff, and abrasion and impact resistant, and are not easily corroded. This is rather a formidable combination of characteristics. Frequently, strong materials are relatively dense; also, increase in their strength or stiffness results in a decrease in impact strength.

Material property combinations and ranges have been, and are yet being, extended by the development of composite materials.  A composite is considered to be any multiphase material that exhibits a significant proportion of properties of both constituent phases such that a better combination of properties is realized. According to this principle of combined action, better property combinations are fashioned by the judicious combination of two or more distinct materials. Property trade-offs are also made for many composites.

Most composites are created to improve mechanical characteristics such as stiffness, toughness, and ambient and high temperature strength. Composites can be simply classifies into three basic categories- particle-reinforced, fiber-reinforced and structural composites.

Generally the matrix is metal or a polymer, due to some amount of ductility that is always desirable. The metal matrix composites (MMCs) can be used at higher service temperatures than their base metal counterparts; furthermore, the reinforcement may improve the stiffness, specific strength, abrasion resistance, creep resistance, thermal conductivity and dimensional stability. High operating temperatures, nonflammability, and greater resistance to degradation by organic fluids are some of the advantages the MMCs provide over PMCs. [7]

The super alloys as well as alloys of aluminium, magnesium, titanium, and copper, are employed as matrix materials. The reinforcement can be in the form of particulates, both continuous and discontinuous fibers and whiskers.

In the reinforcement strengthening in PMCs and to some extent in MMCs, CNTs occupy a primary position due to excellent elastic modulus of 1TPa, tensile strength of 150 GPa and thermal conductivity of 3000-6000 W/mK. [8] Therefore, they can be used as nanofillers to improve mechanical, electrical, thermal properties of composites, unattainable from current materials. Due to its good electrical and thermal conductivity, copper is widely used in electronics and electrical applications. As copper suffers from low strength, different methods are being applied to improve its mechanical properties. Most of these techniques of improving the strength are at the cost of its electrical conductivity. In recent years, researches have adopted CNTs as reinforcement in copper matrix to improve both mechanical as well as electrical properties. However, as the interface between Cu and CNTs are poor, chromium is added to improve its interfacial bonding by the formation of Cr3C2. The carbide transition layer reduces the interfacial energy between Cu and CNTs and in turn improves the load transferability of Cu/CNT composite. [3]

The composite is prepared by milling the three constituents in high energy mill and then consolidating the nano-powder, hence produced, into a single structure. This production technology is referred to as powder metallurgy (P/M). Thus in P/M, the components are manufactured by mixing of metals and non-metal powders, compacting with simultaneous or subsequent heat treatment at higher temperatures using a controlled atmosphere to develop metal or metal like components with satisfactory strength and density. [5]

ADVANTAGES OF POWDER METALLURGY

- Metal plus metal components can be manufactured by P/M. Compositions of any desired composition can be manufactured.

- Metal plus non-metal components can be manufactured, which are quite impossible to manufacture by usual methods.

- Controlled porosity can be obtained in the components. This in essential for certain applications like liquid and gas filters, self-lubricating bearings and insulating bricks.

- It is possible to produce components with the properties similar to their parent metals, which can’t be done my melting and producing alloys.

- Production of refractory metals like W, Th, Mo, etc., is possible without melting.

- Close control over the dimensions of the finished component is easily attained.

Thus, the Cu-Cr-CNT nanocomposite powder was prepared with 1wt% Cr and 0.5wt% CNT by planetary ball milling followed by consolidation through SPS. The consolidated samples were characterized by using SEM for the structural analysis of composite, electrical and mechanical properties.

1.1RAW MATERIAL REQUIRED

The materials required for the experiment are copper, chromium and carbon nano tubes, some properties of which are described below sequentially.

- Copper

Copper is an FCC ductile metal, which is having good electrical conductivity (58 MS/m) thermal conductivity (401 W/mK). Copper, belonging to group 11 of periodic table, has one s-orbital electron on top of a d-electron filled shell and are characterized by high conductivity and ductility. Unlike in metals with filled d-shell, copper does not show covalent behaviour and are relatively weak. This explains the low hardness and high ductility of single crystals of copper.  The thermal conductivity of copper is second highest, highest being that of silver. This is because resistivity to electron transport in metals at room temperature originates by scattering of electrons on thermal vibrations of the lattice, which are relatively weak for a soft metal. [6]

- Chromium

Chromium is a BCC metal with comparatively lower thermal conductivity -93.9 W/mK and electrical conductivity -8 MS/m. It is steel grey in colour, lustrous, hard and brittle material, which takes a high polish, resists tarnishing, and has a high melting point. It has proven of high value due to its high corrosion resistance and hardness. [6]

- Carbon Nano Tubes

Carbon nanotubes (CNTs) are similar to graphite in structure. Each carbon atom is covalently bonded to surrounding three carbon atoms with sp2 hybridization. The difference in the structure is that the layer sheets of graphite are rolled into the cylindrical tube like structure in CNTs. Due to its nm diameter and μm to mm length i.e. large aspect ratio they are called as CNTs. They exhibit excellent thermal conductivity, strength and unique electrical properties. Because of these properties, CNTs are the key element in the fields of nanotechnology, P/M, optics and biomedical etc. Based on the number of walls, CNTS can be classified into-

 Single walled carbon nanotubes

 Multi walled carbon nanotubes

- Single walled carbon nanotubes (SWCNTs):

SWCNTs are the seamless tube structure of one atomic layer of rolled graphite sheet, Fig. 1. These are having diameter of nanometer range and length is million times longer than the diameter. These are mostly used in electronic applications.

Fig. 1: Single Walled CNT.

- Multi walled carbon nanotubes (MWCNTs):

MWCNTs are the cylindrical structure of series of rolled (two or more) graphene sheets. The layers distance between the MWCNTs is in the range of 3.4 Å as like as distance between the graphite layers. These layers are arranged in the concentric cylindrical manner, Fig. 2.

Fig. 2: Multi Walled CNTs.

  - Mechanical milling:

Mechanical milling (MM) / mechanical alloying (MA) is a solid–state powder processing technique involving repeated cold-working, fracturing, and re–welding of powder particles in a high–energy ball mill. The repeated welding, fracturing and rewelding of powder particles can result in intimate mixing of the constituent powder particles on an atomic scale and lead to formation of stable and metastable supersaturated solid solutions, crystalline and quasi–crystalline, a variety of equilibrium and non–equilibrium alloy phases starting from blended elemental or pre–alloyed powders. The mechanical energy transfer to the powder particles in these mills takes place by shear action or impact of the high velocity balls with the powder, as shown schematically in Fig.3.

Fig. 3: Schematic representation of high energy ball milling process

XRD of  coppernanopowder

XRD of  coppernanopowder

. [8]

In a typical case of Cu-CNT composite powder preparation the CNTs were mechanically dispersed into the Cu metal matrix due to repeated collision between the milling media and powder particles.

Various types of mills being used for nanopowders production:

- Ball mill

Ball milling is one of the most widely used. Ball milling consists of placing particle to be ground in  closed cylindrical container with grinding media and rotating the cylinder horizontally on its axis so that the media cascade. This is illustrated schematically in Fig.4. The particles move between the much larger media and between the media and the wall of the mill and are effectively broken into successively smaller particle.

Fig. 4: Schematic representation of ball milling.

- Attritor

- Planetary ball mill

Planetary mills have motion similar to the planets moving around the sun. In this, vials are mounted on the sub disks on the supporting main disk. These two disks have rotary motion about its axis but in opposite direction to each other. This motion is controlled by separate drive mechanism. The centrifugal action from the supporting main disk and vials acts on the material and on the balls in the vials. This centrifugal force acting in and opposite direction in matter in vial leads to grinding balls moving to the bottom of the container and, the matter and grinding media lifting off and move freely over the surface of vials and colliding against the wall. The planetary ball mill used in this composite powder preparation is shown in Fig.5. In this, around 200 g powder can be milled at a time. Fig. 6 shows the mechanism of mill working and the directions in which the vials and the mill moves.

Fig.5: Planetary Mill.

Fig 6: Mechanism of mill operation

- SPEX mill

- Zoz Mill

  - CONSOLIDATION OF POWDER

Spark Plasma Sintering (SPS)

After the powder production and milling or mechanical alloying, the powder particles need to undergo compacting and sintering, before it can be sent for sizing or impregnating and final testing and analysis.

Compacting is one of the most important methods for shaping of metal powders. The powder is fed into a die cavity and the volume is controlled by adjusting the position of the bottom punch in the die cavity. When the die has been evenly filled with powder, the upper surface is levelled and the top punch is pushed into the cavity. The pressure is then applied on any one punch or simultaneously on both the punches to compact the powder. Compacting reduces voids between powder particles and increases the density of compact. However, if the pressing speed is more, the air particles entrapped do not get enough time to escape and therefore remain entrapped only. Due to this subsequent sintering may produce considerable expansion of the compact rather than the usual contraction. Also, a high compaction pressure helps produce a compact of density very near to its theoretical density. But this percentage of theoretical density decreases as the sintering temperature increases.

Sintering is carried out to increase strength and hardness of green compact and consists of heating the compact to some temperature under controlled conditions with or without pressure for a definite time. Sintering process is concerned with diffusion, densification, recrystallization and grain growth. The main driving force behind sintering is the reduction in the free energy due to decrease of surface area. [5]

In conventional methods sintering and compaction are carried out separately and sintering involves heating of the dies which in turn heats the powder inside. However, in case of SPS, this is not true. Here, the compaction and sintering are carried out in one go, where pressure and heat are applied simultaneously. The electric current which flows through the powder ensures heating of the material due to Joule’s heating effect.

SPS is also known as field assisted sintering technique (FAST) or pulsed electric current sintering (PECS). The main characteristic of SPS is that the pulsed DC current directly passes through the graphite die, as well as the powder compact, in case of conductive samples. Therefore, the heat is generated internally, in contrast to the conventional hot pressing, where the heat is provided by external heating elements. This facilitates a very high heating rate (up to ~300 K/min); hence the sintering process generally is very fast (within few minutes). The general speed of the process ensures it has the potential of densifying powders with nano size or nanostructure while avoiding grain coarsening, which accompanies standard densification routes.

The high current pulse energizing method generates:

- Spark plasma

- Joule heating

- An electrical field diffusion effect

The powder particle surfaces are more easily purified and activated than in conventional electrical sintering processes and material transfers at both the micro and macro level are promoted, so a high quality sintered compact is obtained at a lower temperature and in a shorter time than with conventional processes. Conventional electrical hot press uses DC or commercial AC and main factors promoting sintering are:

- Joule heat generated, (I2Rt=H)

- Plastic flow of materials due to pressure.

SPS applies ON-OFF DC pulse voltage and current from a special pulse generator to powder particles. In addition to the two factors for conventional sintering it also discharges between particles of powder occurring at initial stage of pulse energizing for sintering. The sputtering and spark impact pressure eliminates adsorptive gases and impurities from surface of powder particle. Action of electrical field causes high speed diffusion due to high speed of migration of ions. High thermal efficiency is attained because of direct heating of sintering graphite mold and stacked powder materials. SPS can consolidate a homogenous, high quality sintered compact because of uniform heating, surface purification and activation made possible by dispersing the spark points. The sintering dies and punches used in SPS are made of graphite and are subject to Joule heating according to progress of the sintering of the internal powder material, and function as heating elements to assume the role of maintaining homogeneity of the sintering temperature for densification. [1]

MECHANISM

When a spark discharge appears in a gap or at a contact point between particles of a material, a local high temperature state (discharge column) of several to ten thousands of 0C is generated momentarily. This causes evaporation and melting on the surface of powder particles and necks are formed.

Typical examples of materials covered by SPS are:

- Composite materials (Al2O3, TiN, SiC, etc.)

- Ceramics – oxidized and non-oxidized ceramics and cermets(Al2O3+Ni, WC+Co+Fe)

- Super hard alloys

- Amorphous materials

- Magnetic materials

- Intermetallic compounds (TiAl, NiAc, NbCo, NbAl)

- Polymers (polyimide, nylon, polyethylene, etc.)

The schematic of the SPS system which is produced by M/s Sumitomo Coal Mining Co. Ltd., Japan is shown in Fig. 7.

Fig. 7: Schematic representation of SPS.

  - VACUUM FURNACE

A vacuum furnace is capable of heating specimens for various purposes like sintering, annealing, ageing, etc. and at the same time it is capable of maintaining desired conditions inside the heating chamber. We can create a reducing or an inert atmosphere inside the furnace by supplying gases like argon, hydrogen or creating complete vacuum. Thus this furnace enables minimum or no contamination of the samples at all. The vacuum produced is high, of the order of 10-5 mbar. Typical vacuum furnace is shown in Fig. 8.

Specifications of furnace

- Installed power – 31 kW

- Rated capacity (of heating chamber) – 28 kW

- Shut off capacity – 27 ± 2.7 kW

- Nominal temperature in the working space – 2000 0C

- Working space dimension – Width: 100 mm

Length: 300 mm

Height: 100 mm

- Batch weight – 12 ± 0.5 kg

- Working space medium – vacuum

- Ultimate residual pressure in a cold condition of electric furnace – 6.65  10-3 Pa

(5  10-5 mm Hg)

- Rated supply line voltage – 380/220 V

- Current rated frequency – 50 Hz

- Water flow rate for cooling – 1.6 + 0.2 m3/h

- Furnace overall dimension (mm) – Width: 1800

Length: 1450

Height: 1510

- Furnace weight – 1.1 ton

Fig 8: Vacuum furnace

Article components

The furnace is an electric resistance batch-type vacuum furnace with tungsten (W) heaters and screen thermal insulation made of W and Mo and consists of:

- A heating chamber

- Vacuum unit

- A water cooling system

- A furnace transformer

- Control panel

- Microprocessor based controller

The lateral shield of the furnace consists of framework structure on which molybdenum (Mo) card-shields are clamped by means of Mo studs. The lateral thermal insulations have the rounded off angles and slightly converse walls so as to reduce shield distortion in the process of its operation. Electric furnace area is surrounded from sides and both ends by 6 ‘W’-shaped heaters form a tungsten bar, diameter of 6 mm forming the one-phase system from parallel connected groups. The vacuum system consists of:

- A diffusion oil-vapor pump

- Two mechanical pumps (rotary type)

- A vacuum seal

- Four vacuum valves with a hand drive

- A vacuum gate valve with a hand drive

- A leak

For measuring residual pressure in the heating chamber the ionization thermocouple-type vacuum gauge is installed in control desk. Heating element of this furnace is tungsten. In which, refractory is used as metal refractory, which consist of 7 layers. First 3 layers made up of tungsten and remaining layers are made up of molybdenum. The thermocouple used is of type C, consisting of W/W-Re composition. Below table represent the different types of thermocouples. Depending on the required temperature and atmosphere one can choose the type of thermocouple.

Table 1: common thermocouples used in vacuum furnace

| Type | Composition | Max. Temperature (0C) | Atmosphere |
| --- | --- | --- | --- |
| B | Pt-30 Rh/Pt-6 Rh | 1700 | Vacuum, inert, oxidising |
| C | W/W-Re | 2000 | Non-oxidising |
| E | Ni-9 Cr/Cu-44 Ni | 900 | Oxidising |
| J | Fe/Cu-44 Ni | 800 | Oxidising, reducing |
| K | Ni-9Cu/Ni-Mn-Si-Al | 1200 | Oxidising |
| R | Pt/Pt-13Rh | 1500 | Oxidising, inert |
| S | Pt/Pt-10Rh | 1500 | Oxidising, inert |
| T | Cu/Cu-44 Ni | 400 | Oxidising, reducing |

Water cooling system consists of a manifold, a drain funnel, cooling jackets, elements of electric furnace structure and a diffusion oil-vapor pump, connected rubber-cloth hoses clamped to the couplings of water cooling system elements by means of bandings. It is divided into three cooling circuits wherein the water cooled elements of each circuit are connected parallelly.

- A diffusion oil-vapor pump

- Six current leads and a cooler of a heating chamber

- A body and two lids of a heating chamber

On the manifold we have

- A common shut-off valve

- Three valves for cooling circuits

- A pressure gauge for controlling the water pressure at the inlet of the water cooling system.

Requirement for the cooling water quality:

- Hardness of the water – not more than 0.5 mg eq/L

- Amount of suspended matters – not above 5 mg/L

- Water oxidation susceptibility – not above 10 mg/L of O2

- Amount of chlorides – not above 5 mg eq/L

To obtain ideal characteristics of the diffusion oil-vapor pump, the inlet water temperature should not be >20 0C and for other instruments of electric furnace the water outlet temperature should not be >45 0C. Control of water flow rate and consequently water temperature (outlet) is carried out by hand valves. Power supply to the furnace is carried out from the furnace on-phase transformer installed in furnace frame. In control desk installed separately, there are mounted:

- A thyristor voltage regulator

- An instrument transducer

- A microprocessor based controller

- Instrumentation and apparatuses

- Light signal system

Adjustments of the thermal regime are carried out by means of changing the voltage applied. The operation of the electric furnace should be carried out in the following sequence:

- Supply power to the control desk

- Charge a batch

- Carry out the evacuation of heating chamber up to working pressure

- Switch on the heater of electric furnace

- Heat a batch in compliance with the desired schedule

- Cool the batch to room temperature and then supply air to the heating chamber

- Discharge the batch

General rules

The maintenance of the electric furnace should be carried out at the obligatory observance of suitable rules and standards for the service of the electric equipment. During service of electric furnace it is necessary to pay attention to the following:

- Current leads should not be in a contact with metal structures; the distance between the heaters, the thermal insulation and the batch should be strictly kept in conformity with drawings.

- Charge should be cleaned, degreased and dried.

Operations carried out in vacuum furnace

ANNEALING

The cold-worked state is a condition of high internal energy than the undeformed metal. Therefore, there is every possibility of this strain hardened metal to revert back to its stress free state. With increasing temperature the cold-worked condition becomes more and more unstable. Eventually, the metal softens and reverts back to its original strain free condition. The overall process by which this occurs is known as annealing. Commercially, it is a very important technique because it helps to restore ductility of a material which it had lost during cold-working. Therefore, by interposing annealing to severely deformed and strained material, it is possible to restore its ductility and then deform it to a very great extent. The overall process of annealing can be broadly divided into three procedures – recovery, recrystallization and growth.

Recovery can be defined as that phase in which most of the physical properties take their original values without bringing in much change in the microstructure of the material. Electrical conductivity increases and the lattice strains are reduced to a great amount in this phase.

Recrystallization can be defined as the replacement of the old strained grains by a set of new strain free grains. It can be easily detected by the metallographic methods and is evidenced by a decrease in hardness or strength or an increase in ductility.

Grain growth is temperature dependent and grain-coarsening region is soon reached in which the grains grow rapidly. Grain growth is inhibited considerably by a dispersion of a fine dispersion of second phase particles, which restricts the growth of the grain boundaries. [4]

AGEING

Ageing is also a heat treatment technique, in which a sample is allowed to remain at room temperature for some days or at an elevated temperature for a few hours. Usually the latter method is carried out as it is less time consuming.

When a precipitate alloy is quenched, its alloying elements will be trapped in solution, resulting in soft metal. Aging a ‘solutionized’ metal will allow the alloying elements to diffuse through the microstructure and form intermetallic particles. These intermetallic particles will nucleate and fall out of solution and act as a reinforcing phase, thereby increasing the strength of the alloy. Alloys may age ‘naturally’ meaning that the precipitates form at room temperature, or they may age ‘artificially’ when precipitates only form at elevated temperatures. In some applications, naturally aging alloys may be stored in a freezer to prevent hardening until after further operations, which are easier with a softer part. [6]

CHAPTER 02

- Characterization (equipments and techniques)

The characterization of the Cu-Cr-CNT composite was done by four basic equipments:

  - Optical microscope

The metallurgical microscope is the most important tool of a metallurgist. It consists primarily of an objective and an eye-piece. Its primary function is to reveal the details of the object. The clarity and the extent to which the details are revealed depend on the degree to which these optical systems are created.

Principle:  A horizontal beam of light from the light source is reflected by means of a plane glass reflector downwards through the microscope objective on the surface of the specimen. Some of these incident light radiations, reflected from the specimen surface, will be magnified and will pass through the plane glass reflector and get magnified again by upper lens system of the eye-piece.

Constructional details: The table type microscope consists of:

- Stage: A flat movable table supporting specimen. This can be moved up or down by knobs.

- Tube: The vertically movable tube containing eyepiece, objective and a plane glass reflector. The tube length varies from 160 mm to 250 mm.

- Rough & fine focus adjustments - The limbs of microscope carry the coarse & fine adjustments to facilitate focussing of the samples.

- Objective – The body tube carries revolving nose piece carrying the three objectives. This enables quick change of the objective, which helps for a quick resolving the structure of metal.

The important properties of an objective are-

- Magnifying power

2) Resolving power

It is the property by which an objective shows distinctly represented two small adjacent lines in the structure of the object. This is usually expressed as number of lines per mm that can be separated which depends on the numerical operator, the wavelength of the light used. Resolution is particularly important during the microscopy of the micro constituents of metals consisting of fine lamination with core resolution which appears as one uniform area, where as an objective with higher numerical appearance reveals deeper nature of the structure.

- Eyepiece - It is named, as it is near to the eye. It is made up of various powers such as 5, 10, 15 etc.

The basic difference between a biological and metallurgical microscope is the way the sample is illuminated. In biological microscope, the sample, being a biological membrane, usually, is translucent and hence lets the transmission of light take place. Therefore, the microscopy is transmission type. However, in case of metallurgical samples, even if the specimen is very thin, it will not allow light rays to pass through it. This is why we use an external illumination for reflection. Hence, the microscopy is reflection type as shown in Fig.9.

Fig. 9: Optical microscope.

  - Vickers hardness testing

The Vickers hardness test method consists of indenting the test material with a diamond indenter, in the form of a right pyramid with a square base and an angle of 136 degrees between the opposite faces subjected to a load of 1 to 100 kgf. The full load is normally applied for 10 to 15 seconds. The two diagonals of the indentation left on the surface of the material after removal of the load are measured using a microscope and their average value is calculated, Fig. 10. The area of the sloping surface of the indentation is calculated. The Vickers hardness is the quotient obtained by dividing the kgf load by the square mm area of indentation.

Fig. 10: Vickers Hardness Indenter.

The HV number is then determined by the ratio F/A, where F is the force applied to the diamond indenter in kilograms–force and A is the surface area of the resulting indentation in square millimeters. A can be determined by the formula.

(1)

This can be approximated by evaluating the sine term to give

(2)

Where d is the average length of the diagonal left by the indenter in millimeters. Hence

(3)

Where F is in kgf and d is in millimeters.

The corresponding units of HV are then kilograms–force per square millimeter (kgf/mm²).Vickers hardness numbers are reported as xxxHVyy, e.g. 440HV30, where:

- 440 is the hardness number,

- HV gives the hardness scale (Vickers),

- 30 indicates the load used in kgf.

Vickers values are generally independent of the test force: they will come out the same for 500 gf and 50 kgf, as long as the force is at least 200 gf. [8]

  - Scanning electron microscope (SEM)

The scanning electron microscope is a type of electron microscope that produces images of a sample by scanning it with a focussed beam of electrons. The electrons interact with atoms in the sample, producing signals that can be detected and that contain information about the sample’s surface topography and composition. The electron beam is generally scanned in a raster scan pattern, and the beam’s position is combined with the detected signal to produce an image. The most common SEM mode is detection of secondary electrons emitted by atoms excited by the electron beam. The number of secondary electrons depends on the angle at which beam meets the surface of the specimen i.e. on specimen topography. By scanning and collecting the secondary electrons with a special detector, an image displaying the topography of the surface is created.

Principle: There are many other signals that are produce by SEM, which include, back scattered electrons (BSE), characteristic X-rays, light, specimen current and transmitted electrons. These signals result from the interactions that take place between the electron beam and the specimen surface atoms as shown in Fig. 11 and a typical SEM is shown in Fig. 12.

Fig. 11: Various interactions between electron beam and the sample surface.

Fig. 12: Scanning electron microscope.

CONSTRUCTION

The SEM consists broadly of:

  - Electron gun

  - Column of lenses

  - Specimen chamber

  - Secondary electron detector

  - Control console as shown in Fig. 13.

Fig. 13: Schematic representation of SEM.

Electron gun – it is responsible for the production of electron beam, which then interacts with the specimen surface, resulting in various interactions and hence giving us SE, BSE, etc.

- Inside the gun the filament current heats the filament, which then releases electron beam.

- The bias voltage makes the Wehnelt cap repel electrons. This is helpful in confining the electron beam and keeping it focussed.

- The first cross-over point determines the resolution limit of the microscope.

- The probe current is 3 to 4 times smaller than the emission current.

The electron gun is shown schematically in the following Fig. 14.

Fig.14: Electron Gun of SEM.

  - Electrical conductivity measurement

The electrical conductivity of the specimen is measured by the eddy current principle. Eddy currents are induced inside a material when the magnetic field is applied, in a direction perpendicular to the direction of magnetic field. Vice-versa is also true, i.e. when current is allowed to pass through a specimen, magnetic field is produced in its vicinity. A conductive material in contact with this changing magnetic field will conduct electricity and hence produce a secondary magnetic field. Both these fields interact and cause a change in impedance in primary coil. This change in impedance helps us to measure the electrical conductivity of the sample. Fig. 15 shows the conductivity measuring equipment.

Fig. 15: Electrical conductivity measuring device.

CHAPTER 03

- EXPERIMENTAL PROCEDURE

  - Synthesis of Cu-Cr-CNT nanocomposite powder

The nanocomposite powder is prepared in a high energy planetary ball mill with 1 wt% Cr and 0.5 wt% CNT by using ethanol as process control agent (PCA). The PCA helps to avoid sticking of the powder particles to the vials as well as to the balls. The milling takes about 12 to 2 4 hr. The composite powder is reddish in colour due to copper being the basic component. The as prepared sample might pick up some oxygen and so needs a reduction.

  - Reduction of nanocomposite powder

As the powder picks up oxygen from the atmospheric contamination, the powder needs to be reduced to get phase pure form. This is done in a vacuum furnace. After vacuum creation, the chamber is back filled with hydrogen gas and the sample powder was heated up to 600 0C at a slow rate of 3 0C/min. This is done while keeping up with the kinetics of the reduction reaction between the CuO and H2. Entire reduction is carried out under a continuous flow of hydrogen gas. Hydrogen reacts with CuO to produce H2O and Cu powder, as follows

CuO (s) + H2 (g) = Cu (s) + H2O (g)

Table 2: parameters of vacuum furnace while copper reduction.

| Temperature | 600 0C |
| --- | --- |
| Soaking time | 1 hr |
| Pressure of diffusion pump | 0.045 mbar |
| Current | 0.4 - 0.6 kA |
| Pressure inside furnace | 0.2 kgf/cm2 |

The pressure inside furnace is controlled manually by controlling the inlet and the outlet pressure of the gases. The powder obtained has a cake like appearance and is crushed in a pestle and mortar before sintering.

  - Sintering of powder (SPS)

-Take about 80 g of composite powder for sintering.

-Put the powder in the graphite die. There are punches at both the ends of the graphite die. We also use graphite sheets, so as to ensure that the powder does not

Stick to the punch surface and damage it.

-Minor load of 1N is applied to make a strong contact between the constituents inside the die.

-Like the vacuum furnace, the SPS also has two pumps – ‘rotary’ and ‘booster pump’.

-SPS also needs creation of vacuum prior to the sintering process. The pressure of 6 to 8 Pa is achieved as measured on the vacuum gauge or the chamber pressure gauge.

-The heating rate is high in SPS, which can go up to 500 0C/minute. However, we maintain a rate of 100 0C/min for 9 min.

-The powder was taken to of 900 0C under a minimum load of 1 N and cooled to 650 0C, where a pressure of 75 MPa is applied.

  - Solutionizing treatment

-Put the as-prepared samples in the vacuum furnace.

-Before the annealing is started, the furnace needs to be evacuated of the air or any other gases present inside the chamber. Evacuation process is completed in 2 hr.

-The first evacuation is done till we achieve a pressure of 10-1 mbar, using rotor pump. When the minimum pressure is attained, then evacuation using diffusion pump takes place for 45 min. As the pump is oil-vapour type, it requires water cooling.

-Set the temperature to 980 0C on the control panel.

-When the overall pressure of 0.001 mbar is achieved, start heating at the rate of

100C/min. till a temperature of 980 0C is achieved. This takes about 1hr 40 min. Pre-set the soaking time as 1hr.

-As the temperature increases, we observe a wide difference in set temperature and process temperature, which in turn changes the current input. This is observed until we attain a temperature of ~300 0C. After this the temperatures become stable.

(Note – set temp: temperature that the furnace should have attained by that time

Process temp: temp inside the furnace.

If Set temp is more, the power/current input increases

If process temp is more, the current input reduces.)

-When the temperature reaches 980 0C, it will stop further heating due to already set data. It will be maintained at that temperature for 1 hr soaking.

-After soaking, close the valves for hydrogen input and let the furnace cool to ambient temperature.

-The annealed samples can then be taken for characterization of their mechanical and physical properties.

The heat treatment graph obtained is as follows:

Fig 16: Heating schedule followed for solutionizing treatment.

  - Ageing

-Some of the samples, which have already been annealed, are treated again by this heat treatment method.

-Some of the samples are heated to two selected temperatures of 400 0C and 600 0C at a heating rate of 100C/min and were held for 1 hr at that temperature and furnace cooled.

-The cooling rate in ageing is much slower than that in annealing. This is because of the hydrogen atmosphere in annealing and vacuum in ageing.

Therefore, we have obtained four different types of samples: sintered samples, annealed samples, aged samples at 400 0C and aged samples at 600 0C. Now these samples are to be tested for different properties by different methods, as mentioned:

  - Conductivity measurement

Electrical conductivity of the material is measured with the help of the instrument mentioned in chapter 02. The samples do not require any special preparation. Rough polishing of the sample is required on emery paper so as to remove the oxide layer. This layer otherwise brings in insulation effects and does not give exact values of conductivity. The polished specimens are placed on a float surface and their conductivity is measured.

  - Metallographic specimen preparation

Other than conductivity, we also need to find out hardness value of the specimens and characterize them using SEM. This requires complete metallographic preparation of the samples.

-Due to the awkward shape of the samples, they are mounted in the mounting press using bakelite powder.

-The specifications during mounting are:

Heating time: 10 min

Heating current: 5 A

Heating temperature: 170 0C

Cooling time: 5 min

Pneumatic pressure: 50 psi

-The mounted samples are then polished on emery papers starting from number 200, 400, 600, 800 and then finally on 1000 grit sizes. These papers have SiC grains on their surface, which are responsible for the grinding action. This is dry polishing.

-Dry polishing is followed by wet polishing. This is done on an ‘automatic polishing unit’. In wet polishing, polishing disks made of brass, covered with velvet cloth, and liquid abrasives are used. The samples are fitted in the holder and a ‘polycrystalline diamond suspension’ is sprayed on the disk while it rotates.

Three suspensions of size 3µm, 6µ and 9µm were used, going from 9 to 3.

The specifications are:

Speed of the head: 40 rpm

Time: 18 min

-After final wet polishing by 3 µm diamond suspension, the polished specimens are taken for ultrasonication. Samples are individually placed in beakers filled with acetone, in a position that the composite surface faces the beaker wall. The beakers are then placed in the sonicator for 5 min. Ultrasonication ensures the removal of diamond particles, if any, on the sample surface. These particles can otherwise trample the hardness values of the composite, pertaining to the fact that diamond is the hardest material.

-After sonication, the samples need to be washed with acetone followed by low drying using a hair dryer. The samples are ready for microhardness test.

-For SEM, the samples after undergoing microhardness test need to be polished with ‘alumina 0.05 micron suspension’. This is also done in the automatic polishing unit.

Specifications:

Time: 1 hr

Head speed: 30 rpm

During the polishing operation, we add 4-5 drops of alumina suspension after 5-10 min interval.

The rate of water supply is fixed.

Towards the end of the alumina polishing, for nearly 10 min no alumina is added and water supply is increased. This cleanses the disk and the sample of the alumina suspension. The specimen is washed with acetone and dried.

-Following polishing the samples are etched with nital solution (2% HNO3 and 98% ethanol). The specimen is viewed under optical microscope for the grain structure appearance. As the grains spear, the specimens can undergo SEM imaging.

  - Microhardness measurement

This is carried out on the automated indenter. The indenter makes an indent on the surface using a square based diamond indenter. The diagonal lengths are measured and the hardness number can be calculated as shown in Fig. 17.

Fig. 17: Indent created by Diamond indenter.

  - SEM characterization

The samples are characterized using SEM for analysing the chemical composition and the topography of the samples. The conducting part of the surface of composite is connected to the bottom part of the bakelite, such that when we keep it on the platform the conducting tape touches the plate, which also is conducting. The tape is used because the bakelite portion of the mount is insulating and will not let the electron beam pass through it.

The chamber is first evacuated of air, which takes about 2-3 min and then electron beam is allowed to strike the surface. The resultant X – rays, secondary electrons and the back scattered electrons are analysed for composition and the topography of the sample. This enables us to get an idea about the grains and the distribution of chromium and CNT in the copper matrix.

CHAPTER 04

- RESULTS

  - Electrical conductivity

The electrical conductivity values for the samples at room temperature were measured as follows and the values are shown in Table 3 and Fig. 19.

Table 3 Conductivity of Cu-Cr-CNT composite samples.

| Sample type | Conductivity (σ), MS/m |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | σ1 | σ2 | σ3 | σ4 | σ5 | σavg |
| SPS | 34.46 | 34.34 | 34.32 | 34.6 | 34.52 | 34.45 |
| Annealed at 900 0C | 18.28 | 18.20 | 17.89 | 18.04 | 18.24 | 18.13 |
| Aged at 400 0C | 19.85 | 19.76 | 19.76 | 19.8 | 19.63 | 19.76 |
| Aged at 600 0C | 28.69 | 28.25 | 28.08 | 28.57 | 26.80 | 28.07 |

Fig. 18: Trend of conductivity values.

In the figure:

Sample 1- SP Sintered

Sample 2- Annealed at 900 0C

Sample 3- Aged at 400 0C

Sample 4- Aged at 600 0C

  - Micro hardness

The micro hardness values and the length of the diagonals for the samples as measured by the Vickers indenter machine are shown in Table 4 for as-sintered samples.

SPS Sample

Table 4: Hardness of SPS sample.

| S.No. | D1 (µm) | D2 (µm) | HV |
| --- | --- | --- | --- |
| 01 | 29.3 | 29.1 | 108.74 |
| 02 | 29.5 | 29.2 | 107.64 |
| 03 | 28.8 | 28.4 | 113.36 |
| 04 | 29.0 | 28.7 | 111.4 |
| 05 | 29.1 | 28.9 | 109.49 |

The hardness of sintered sample is 110 HV0.05

For the annealed sample the values are shown in Table 5.

Table 5: Hardness of annealed sample.

| S.No. | D1 (µm) | D2 (µm) | Hv |
| --- | --- | --- | --- |
| 01 | 35 | 35.1 | 75.47 |
| 02 | 34.6 | 35.6 | 75.27 |
| 03 | 35 | 34.6 | 76.56 |
| 04 | 35 | 35.3 | 75.05 |
| 05 | 34.6 | 34.9 | 76.78 |

The hardness of annealed sample is 76 HV0.05.

For the aged sample (at 400 0C), the values are shown in Table 6.

Table 6: Hardness of aged sample at 400 0C.

| S.No. | D1 (µm) | D2 (µm) | Hv |
| --- | --- | --- | --- |
| 01 | 37.8 | 37.4 | 65.58 |
| 02 | 39.5 | 38.3 | 61.27 |
| 03 | 38.5 | 37.9 | 63.57 |
| 04 | 38.1 | 37.4 | 65.05 |
| 05 | 38.6 | 37.4 | 64.21 |

The hardness of sample aged at 400 0C is 64 HV0.05

For the aged sample at 600 0C, the hardness values are shown in Table 7.

Table 7: Hardness of aged sample at 600 0C.

| S.No. | D1 (µm) | D2 (µm) | Hv |
| --- | --- | --- | --- |
| 01 | 30 | 29.2 | 105.83 |
| 02 | 30 | 29.7 | 104.06 |
| 03 | 29.5 | 28.6 | 109.87 |
| 04 | 29.6 | 28.9 | 108.37 |
| 05 | 29.6 | 29.4 | 106.54 |

The hardness of sample aged at 600 0C is 107 HV0.05

The variation in hardness is schematically shown in Fig. 19.

Fig. 19: Variation of micro hardness with the sample history.

In the figure:

Sample 1- SPS sample

Sample 2- Annealed at 900 0C

Sample 3- Aged at 400 0C

Sample 4- Aged at 600 0C

  - Microstructure analysis

After analysing the sample under SEM we get following images,

(a)

(b)

(c)

(d)

Fig 20: (a) SPS sample, (b) Solutionized sample, (c) Aged sample (400 0C),

(d) Aged sample (600 0C).

CHAPTER 05

- DISCUSSIONS

- The conductivity of fully annealed copper is 58 MS/m and that of sintered composite observed in this case is 34 MS/m. It drastically reduces to 18 MS/m after annealing. However, on ageing at 400 0C we can increase it to ~20 MS/m. Increasing the ageing temperature to 600 0C increases its conductivity value to 28 MS/m. It may be presumed here that the dissolved chromium in copper could be the reason for the reduction in the electrical conductivity upon annealing treatment. The samples upon ageing treatment get the chromium from the solution into precipitates so that the electrical conductivity increases.

- Hardness value increases from 90 HV0.05 for sintered copper powder to 110HV0.05 for SPS composite, thus increasing its strength. The value reduces upon annealing to 76 HV0.05, thus making the composite ductile. It becomes more ductile on ageing to 400 0C as its hardness reduces to 64 HV. On the contrary, it hardens when aged to 600 0C with its hardness value increasing to 107. The reduction in hardness and the sample attaining lost ductility after sintering upon annealing could probably due to again chromium going into the solution of copper which would have been occupying the grain boundaries earlier. However, the decrease in hardness is to be understood. The samples upon ageing at different temperatures would bring the dissolved chromium into the fine precipitates thus giving rise to increase in hardness.

- The grain size increases as we go from SPS to annealed to aged samples. The sintered sample shows minimum porosity and hence highest conductivity. The porosity increases as the sample is solutionized. However, aging the samples to higher temperatures again reduces its porosity, thus providing better conductivity. Also we observe a lot of twins that appear after annealing. Twin boundaries play a good role in enhancing conductivity properties. [9]

CHAPTER 06

- CONCLUSIONS

- The conductivity of the material decreases, but the value still retains 51% of its conductivity which can further increase to 60% upon further heat treatment. The reduction of the property value from that of copper can be possibly due to improper distribution of the reinforcing CNT. However, the conductivity increases on heat treating the sample. This can be due to increase in the grain size and hence reduction in the number of grain boundaries.

- The hardness of the sintered composite is more than that of sintered copper. It increases by about 22.22%. This can be related to the reinforcement. Since the brittleness of the material makes it unfit for usage, the heat treated sample becomes ductile. In order to get better strength and ductility we again have to increase the ageing temperature or the ageing time. By doing so, the hardness showed a considerable increment.

- Sintered samples show high conductivity and at the same time are too brittle for practical applications. Heat treatment of the samples helps to maintain both the properties at the same time - conductivity and strength. Even though the porosity increases as compared to that found in sintered samples, but the twin boundaries, the conducting reinforcement and the heat treatment seem to overpower them and result in an overall increase in porosity. However, a combination of sintering, solutionizing and ageing treatments seem to give the Cu-Cr-CNT composite an added advantage of improved hardness with a conductivity of 60% (international annealed copper standard (IACS)).

REFRENCES

- ‘Mechanism of spark plasma sintering’. Tokita,Sumltomo Coal Mlmng Company, Ltd.East Bldg. 108, Kanagawa Science Park KSP 2-1, Sakato 3-chome, Takatsu-ku, Kawasaki-shi Kanagawa 213 Japan .

- ‘Investigation on solid solubility and physical properties of Cu-Fe/CNT nano-composite prepared via mechanical alloyed route’. M. BarzegarVishlaght, A. Ataie. School of metallurgy and Materials Engineering, University of Tehran, Tehran, Iran.

- Improvement of interface and mechanical properties in carbon nanotube reinforced

Cu–Cr matrix composites’.

Ke Chu (a), Cheng-changJia(b), Li-kun Jiang (b), Wen-sheng Li (a)

- State Key Laboratory of Gansu Advanced Non-ferrous Metal Materials,

Lanzhou University of Technology, Lanzhou 730050, China

- School of Material Science and Engineering, University of Science and

Technology Beijing, Beijing 100083, China

- ‘Mechanical Metallurgy’- by George E. Dieter

- ‘Materials Science and Metallurgy’ - by Kodgire

- Wikipedia

- ‘Materials and metallurgy’- by William D. Callister.

- M.Tech Thesis by Gorli Siva Kumar, on ‘Cu–Cr–CNT Composites through High Energy Ball Milling and Spark Plasma Sintering’.

- ‘Ultrahigh Strength and High Electrical Conductivity in Copper’ Lei Lu, Yongfeng Shen, Xianhua Chen, Lihua Qian, K. Lu*